## Slide 1
Quantum Anomalous Hall Effect and Majorana Fermion
Department of Physics
Tsinghua University (清华大学)
Qi-Kun Xue
“Topology in Condensed Matter and High Energy Physics”, Croucher Advanced Study Institute,
The Chinese University of Hong Kong, Jan. 3-5, 2018

## Slide 2
Introduction
MBE growth of topological insulators
Quantum Anomalous Hall Effect
New developments and summary
OUTLINE

## Slide 3
1879
Hall Effect
E. Hall
H
RH
1881
Anomalous HE
H
RH
2016
Topological Phase Transitions and Topological Phases of Matter
D. Thouless
F. Haldane
J. Kosterlitz
Quantization of AHE?
H
RH
h/e2
h/2e2
1980
IQHE (Si)
1982
FQHE
(GaAs)
RH=3h/e2
1983
TPM
K. von Klitzing
D. Tsui
B. Laughlin
H. Stormer
1998
1985
IQHE
FQHE
2010
Half-integer
QHE
(graphene)
2005

## Slide 4
The first Theoretical Proposal for Quantum Hall Effect
without Magnetic Field
Graphene with broken TRS
Science 329, 61 (2010).
Page 2018:
While the particular model presented here is unlikely to be directly physically realizable, at least in principle, QHE does not necessarily require external magnetic fields……

## Slide 5
Conductor
Insulator
Classification of a Material (new)
Topological
Insulator
Insulating (bulk)
conducting (surface)
Spin-Orbital Coupling
Notes: We started this study last year. By standard MBE film growth technique, we could prepare TI films with LBL thickness control.

## Slide 6: Ordinary versus Topological Insulators
Valence Band
Conduction Band
Rashba Spin-Orbit Splitting of Surface States
Valence Band
Conduction Band
Ordinary Insulator
Time reversal symmetry, Strong S-O coupling
Spin up
Spin down
Strong spin-orbit coupling
Topological Insulator
“band twisting”
kx
ky
E
(m=0)
Notes: Let’s first talk about TI. In this slide, I show you the difference between ordinary insulator and topological insulator. This is the band structure of a normal insulator, the valence band, the conduction band, and the energy gap between. If the gap is not large, and the spin-orbital coupling in the material is very strong, then there will be a band twisting. The band twisting produces linearly dispersed and spin-polarized bands within the gap. The states are very robust unless the time-reversal symmetry of the system is broken because of the Kramers degeneracy.
Therefore, the band topology is very different.
In real space, TI can be regarded as a bulk-insulating narrow-band semiconductor with metallic states on its surface or boundary.

## Slide 7
Theories for QHE without a magnetic field
Spin-orbital coupling + magnetism
Onoda, Sugimoto & Nagaosa, PRL 97, 126602 (2006)
X. L. Qi, Y. S. Wu, S. C. Zhang, PRB 74, 085308 (2006)
Z. Qiao, Q. Niu et al., PRB 82, 161414(R) (2010)……
“Quantum Anomalous Hall Effect” by Naoto Nagaosa
QAH
Notes: A question is that is it possible to realize QHE without magnetic field. Or in other words, is it possible to find an topological insulator without magnetic field? The answer is yes. In 1988, Haldane propose a mode, which is basically a graphene but with its time reversal symmetry broken somehow. We know the energy band of graphene is a Dirac cone. By breaking its TRS, the Dirac cone will be gapped and become an insulator. Such an insulator is an topological insulator with Chern number of 1. Thus we can observe QHE in this system without Landau levels. It means QHE can appear without magnetic field and high sample mobility, which will be good at application of QHE. Unfortunately, the graphene with broken TRS is difficult to realize. Little progress has been made in this direction.

## Slide 8
Hg1-yMnyTe QWs
C. X. Liu et al. PRL101, 146802 (2008)
Theory: making TIs ferro-magnetic
TI/Magnetic layer
X. L. Qi et al., PRB 78, 195424 (2008)
Gapped Dirac surface state:
a QH insulator: sxy = 1/2 (e2/h)
II
3D TI with FM
M
Thin film with FM
M
Film edge: topological edge (a domain wall)
Opposite z: different topological number
S.-Y. Xu et al., Nat. Phys. 2012
SP-ARPES: Δ + z-polarization
Magnetic doped Bi2Se3 family
R. Yu et al., Science 329, 61 (2010)
Magnetic doping (Bi2Se3/Bi2Te3/Sb2Te3)
Y. Z. Li et al., Nat. Phys. 6, 284 (2010)
Notes: If we introduce ferromagnetism in a 3D TI, the broken TRS will open a gap at the Dirac surface states. Such a gap-opening was reported in spin-resolved ARPES. The gapped Dirac surface states is actually a QH insulator with half QH conductance. To measure the QH conductance we need to produce an edge. However, the surface states of a 3D TI with closed surface has no edge.
To produce the edge, we just reduce the film thickness. Since the top and bottom surfaces have different topological character, the film edge becomes a topological edge, and carry a full quantum conductance--e2/h.

## Slide 9
Zhang et al., Nat. Phys. 5, 438 (2009)
Xia et al., Nat. Phys. 5, 398 (2009)
Sb2Te3
Bi2Te3
Bi2Se3
Bi2Se3
3D Topological Insulators: Bi2Se3, Bi2Te3, Sb2Te3
300 meV
Se
Bi
Notes: The experiment in our group was done with 3D TI, BiSe----SbTe, so, today we focus on the three materials, which were first studied by Prof. Zhang and Prof. Hasan’s groups.

## Slide 10
Z. X. Shen: Science 2009
Bi2Te3
Bi2Se3
Dirac Cone
Hasan: Nat. Phys. 2009
Electron Band Structure of 3D TI by ARPES
n-type conductor
(Se vacancies)
(Similar to that in ZnO)

## Slide 11: Topological Insulator Material
“insulator” by definition: Bulk insulating
Surface metallic (2D)
(real space)
bulk
High quality:
low defect/impurity density
If the bulk is conducting, it is difficult to measure the transport property of its surface with exotic topological property.
Notes: Let’s first talk about TI. In this slide, I show you the difference between ordinary insulator and topological insulator. This is the band structure of a normal insulator, the valence band, the conduction band, and the energy gap between. If the gap is not large, and the spin-orbital coupling in the material is very strong, then there will be a band twisting. The band twisting produces linearly dispersed and spin-polarized bands within the gap. The states are very robust unless the time-reversal symmetry of the system is broken because of the Kramers degeneracy.
Therefore, the band topology is very different.
In real space, TI can be regarded as a bulk-insulating narrow-band semiconductor with metallic states on its surface or boundary.

## Slide 12
Molecular Beam Epitaxy (MBE) (Cho & Arthur, 1970)
Atomic-Level
Scanning Tunneling Microscope (STM)
(Binnig & Rohrer, 1981)
Ek : kinetic energy
hu : photon energy
W : work function
Ek = hu – W – E (k//)
E(k//): band dispersion
Angle-Resolved Photoemission Spectroscopy (ARPES)
Ultra-High Vacuum Systems
Notes: Yesterday, we heard of lot of beautiful story about the history of MBE. Particularly from Dr. Cho, a pioneer of MBE, we know that MBE was formally termed in 1970. Everybody here knows well that MBE is one of the most powerful techniques for preparing high quality film materials. If we further combine MBE with STM and ARPES, we can control the film growth at atomic level, we can study atomic and electronic structure and band structure atomic-layer-by-atomic-layer. My group has been working this kind study about 10 years go.

## Slide 13
UHV MBE-STM-ARPES
STM
MBE
ARPES
Omicron + VG Scienta

## Slide 14
20ML Pb
Ji etal., PRL 100, 226801 (2008)
Chen et al., PRL 101, 197208 (2008)
Fu et al., PRL 103, 257202 (2009)
Zhang et al., PRL 103, 266803 (2009)
UHV LT High-Magnetic Field STM-MBE
T: 400 mK, B: 11 T
UHV: 5x10-11 Torr
Unisoku

## Slide 15
Introduction
MBE growth of topological insulators
Quantum Anomalous Hall Effect
New developments and summary
OUTLINE

## Slide 16
Growth Kinetics
GaAs
TGa > TSub > TAs
As-rich:
As4/Ga>30
Qi-Kun Xue et al., Phys. Rev. Lett. 1994, 1995
Qi-Kun Xue and T. Sakurai, MBE-STM of III-V Compound Semiconductors, Progress in Surface Science 57, 1-132 (1997)
GaAs = Ga + As4
Bi2Se3
TBi > TSub > TSe
Se-rich:
Se2/4/Bi>20
(Bi2Te3)
Bi2Se3 = Bi + Se2/4

## Slide 17
Establishment of MBE growth conditions
RHEED
Real time RHEED intensity oscillation
TBi >> TSub > TSe
High VI (Se) flux
Bi2Se3:
Y. Y. Li et al., Adv. Mater. 2010
Stoichiometric: low impurities
Layer-by-layer: flat & single crystalline
1QL
Notes: By optimization of the growth conditions, we could be able to achieve LBL growth of the films, as evidenced by the real-time oscillation. One circle of oscillation corresponds to one atomic layer growth, like this.

## Slide 18
STM: atomically flat Bi2Se3 films on graphene
200 nm x 200 nm
-120mV
50 QL
Yi Zhang et al., Nature Physics 6, 584 (2010)

## Slide 19: Bi2Se3 Band Structure: layer-by-layer
Figure 2
k// (Å-1)
k// (Å-1)
k// (Å-1)
3 QL
5 QL
6 QL
Binding Energy (eV)
1QL
2 QL
k// (Å-1)
EF
k// (Å-1)
1 QL
Yi Zhang et al., Nature Phys. 6, 584 (2010)
The thickness and band structure can be controlled with atomic-layer precision by MBE
Applied to FeSe, MoSe2 and other layered materials
Critical thickness

## Slide 20
APRES test for thin Bi2Se3 film grown on graphene SiC surface
Binding Energy (eV)
k// (Å-1)
k// (Å-1)
k// (Å-1)
k// (Å-1)
k// (Å-1)
EF
7QL
8QL
9QL
10QL
15QL
50QL
Binding Energy (eV)
EF
k// (Å-1)
Position of Dirac Point
Gap size

## Slide 21
STM: atomically flat Bi2Te3 films
Y. Y. Li et al., Adv. Mater. (2010)
G. Wang et al., Adv. Mater. (2011)
X. Chen et al., Adv. Mater. (2011)
16 nm x 16 nm
Te atom
Notes: The STM images demonstrate the atomically flat property of our films. In 200x200, only three atomc steps can be seen. From the high resolution image here, we can see individual Se atoms. Clearly there are very few defects, compared with previous study.

## Slide 22
kx
ky
E
EF
ARPES: Bi2Te3 band structure
Bi2Te3
Si substrate
Experimentally confirmed：
Massless Dirac Cone
Insulating topological insulator

## Slide 23: Sb2Te3
Y. P. Jiang, PRL 108, 016401 (2012)
Y. P. Jiang PRL 108, 066809 (2012)
0.5 m x 0.5 m

## Slide 24
STM study of fundamental properties of TIs
0
1
2
3
4
6
5
8
7
9
10
11
12
B = 10T
Quantum Interference
Zhang et al., PRL 103, 266803 (2009)
Cheng et al., PRL 105, 076801 (2010)
Absence of backscattering
Jiang et al., PRL 108, 016401 (2012)
Jiang et al., PRL 108, 066809 (2012)
Massless Dirac fermion
(Landau Quantization)
Chang et al., PRL 115, 066809 (2015)
Song et al., PRL 114, 176602 (2015)
New TIs

## Slide 25
We were able to prepare high quality epitaxial thin films of topological insulators by MBE
Notes: Different from most people here, my group use MBE combined STM and ARPES on two very important directions in condensed matter physics: topological insulator and high temperature superconductivity.
IN THIS TALK, I would show you the experimental observation of quantized anomalous Hall effect, means quantum Hall without magnetic field, and interface enhanced superconductivity with a Tc most likely higher than 77K, which is very exciting.

## Slide 26
Band structure of pure Bi2Te3 or Sb2Te3
EF
Bi2Te3
EF
Sb2Te3
Bi2Te3: n-type, DP in valence band
Sb2Te3: p-type, DP in gap
EF
Bi2Te3 + Sb2Te3
DP at gap
Bulk insulating
Notes: First 3D TI Bi0.9Sb0.1
Question: is any arbitrary alloy also a TI? Is it is true, how the Dirac surface band evolve with alloying

## Slide 27
J. S. Zhang et al., Nat. Commun. 2, 574 (2011)
Band engineering of (Bi1-xSbx)2Te3
1. The band topology is preserved in all compositions
2. Charge neutral point (DP = EF): x = 0.95 (Sb)
n to p transition

## Slide 28
Correct Band structure
(BixSb1-x)2Te3
bulk insulating
ferromagnetic topological insulator
High quality material

## Slide 29
Resistivity vs Doping
Queisser and Haller, Science 1998
One donor per million Si atoms
Heavily doped
One donor per billion Si atoms
Intrinsic
Ultra-pure
Gold
Siliver, Copper
Diamond
Nickle oxide
Glass
Silver bromide
104
102
100
10-2
One dopant/impurity per 106 atoms
105 to 10-2 Ωcm
(Bi0.1Sb0.9)2Te3: Δ < 0.15 eV
Si: Δ =1.14 eV
Notes: In this slide, I give a comparison between semiconductor and superconductor, in terms of the material quality. Taking Si, the most advanced semiconductor material, as an example. Now one can achieve crystal quality with defect density as low as 10^(3 to 4) out of the bulk density of 10^(23). One can purify the material up to 10 nines easily. Equally importantly, one can control the doping concentration very very precisely. The right panel gives the resistivity of Si as a function of doping level, published in Science in 1998 by these two authors. Here is diamond, which is very insulating and has a resistivity of 10^(14) Ohm-centimeter. Here is gold, the best conductive metal, which has a resistivity of 10^(-6).
For intrinsic Si without doping, the resistivity is 10^(5). As you can see clearly here, only by doping one carrier per million Si atoms, the resistivity drops to 10^(-2), change by seven orders of magnitude.
Such kind quality and such kind control account for the big success of Si semiconductor technology, which you can find in every computer of you.

## Slide 30
Introduction
MBE growth of topological insulators
Quantum Anomalous Hall Effect
New developments and summary
OUTLINE

## Slide 31
Cr/Fe doped Bi2Se3 (Δ = 0.30 eV)
Yu et al., Science 329, 61 (2010)
Magnetic doping
J. S. Zhang et al., Science 339, 1582 (2013)
Cr: 11%
WL-WAL
Topology-driven quantum magnetic phase transition
paramagnetic

## Slide 32
Cr doping of (Bi,Sb)2Te3
1 QL
Te
Bi(Sb)
Te
Bi(Sb)
Te
(1.0 nm)
Cr substitutes Bi(Sb)
not introduce additional carriers: insulating
No Cr clustering (Mn-GaAs)
Correct Cr concentration
too little: no FM ordering
too much: destroy band topology
QAHE: growing insulating ferromagnetic TIs

## Slide 33
Low temperature MBE growth of (BiSb)2Te3 and Cr doping at 180 C
1. Cr at Bi or Sb site
2. no Cr clustering
C. Z. Chang et al., Adv. Mater. 2013

## Slide 34
Magnetic property: independent of doping
Bi content (x)
Curie temperature (K)
Chang et al., Adv. Mater. 2013
Ferromagnetic phase (even at zero carrier density)
0
van Vleck mechanism?……
J. Y. Zhu: different explanation

## Slide 35
Quantum Anomalous Hall Effect in Cr0.15(Bi0.1Sb0.9)1.85Te3
-55 V
220 V
0 V
30 mK
experiment
20 samples at T = 1.5 K
6 samples at T = 90 mK (zero-field  = 0.87 to 0.98 h/e2)
2 samples at T = 30 mK (full quantization at h/e2)
C. Z. Chang et al., Science 340, 167 (2013)
-1.5 V
At different gate voltage, nearly no change in the shape and coercivity.
(van Vleck mechanism)
2. yx is nearly independent of H.
(perfect ferromagnetic ordering and charge neutrality)
3. At -1.5V, yx = h/e2
H
h/e2
theory
0
Notes: Left figure shows Hall sheet resistance as function of magnetic field perpendicular to the film.

## Slide 36
2014.08： Tokyo/RIKEM
2014.09：UCLA
2015.03：MIT
2015.05: Stanford
2017.06: Wurzburg
2016.06: Princeton
Confirmation of QAHE

## Slide 37
1879
Hall Effect
E. Hall
H
RH
1881
Anomalous HE
H
RH
2016
Topological Phase Transitions & Topological Phases of Matter
D. Thouless
F. Haldane
J. Kosterlitz
2013
h/e2
H
RH
QAHE
H
RH
h/e2
h/2e2
1980
IQHE (Si)
1982
FQHE
(GaAs)
RH=3h/e2
1983
TPM
K. von Klitzing
D. Tsui
B. Laughlin
H. Stormer
1998
1985
IQHE
FQHE
2010
Half-integer
QHE
(graphene)
2005
Completion of the quantization of all Hall effects
Cr0.15(Bi0.1Sb0.9)1.85Te3

## Slide 39
April 12, 2013

## Slide 40
Introduction
MBE growth of topological insulators
Quantum Anomalous Hall Effect
New developments and summary
OUTLINE

## Slide 41
QAHE: < 50 mK
Temperature: a key factor for applications
Magnetic proximity
Higher quality TI materials
Co-doping or other dopants
……
Notes: Later the QAHE was also observed by other groups. But for all the experiments the temperature required to observe full quantization is below 100 K. So such a low temperature is needed? To answer the question, we can check the factors determining the QAHE. 。。。。Actually all the factors can be tuned by the thickness of magnetic TI films. So we may find the key factor determining temperature of the QAHE by studying thickness dependence of the QAHE.

## Slide 42: “Penta-layer” Cr-doped (Bi,Sb)2Te3
Good quantization
at 0.5 K and zero field
Y. Tokura: APL 107, 182401 (2015)
Notes: Actually, recently, Tokura group reports an increase of the QAH temperature in so-called pentalayer structure. It is essentially a sandwich structure with heavily Cr doped (Bi,Sb)2Te3 as FMI layers.

## Slide 43
MIT/PSU/Stanford
V-doped Sb2Te3
Quantized Anomalous Hall Effect in V-Sb2Te3
(~4%)
Dr. Chang and Prof. Moodera (MIT)
25 mK

## Slide 44: Cr & V co-doped (Bi,Sb)2Te3 films
@ 1.5 K
5 QL (CryV1-y)0.19(BixSb1-x)1.81Te3
Cr:V
Notes: Very recently we found that by co-doping V and Cr, we can increase the QAH temperature. Left side is Cr doped, and right side is V-doped. We can see that at an optimized Cr:V ratio, we can get rho_yx of 0.97 h/e2 at zero magnetic field at 1.5 K.

## Slide 45: Full quantization at 0.3 K
b
a
Y. B. Ou et al., APL Materials 4, 086101 (2016)
Notes: At 0.3 K, we get perfect quantization (rho_xx is below 200 Ohm)

## Slide 46
Z. Y. Zhang, S. B. Zhang, E. Kaxiras: Phys. Rev. Lett. 117, 056804 (216)
V and I coped Sb2Te3
T = 50 K
Notes: Next we shall consider to develop QAH-based QAH devices. The first step is to control, for example to turn on/off the chiral edge states with magnetic or electrical way. Since QAH phase is determined by ferromagnetism the magnetic way is easier.
If we could control the relative magnetization of the top and bottom surfaces we can turn on/off the edge states. In parallel configuration we get the QAH phase. In anti-parallel configuration the edge states will be turned off. It is actually a so-called axion insulator phase.

## Slide 47
Creating Majorana modes in TIs
NbSe2
Bi2Te3
  †
Xu et al., PRL 114 017001 (2015)
Sun et al., PRL 116 257003 (2016)
Majorana zero modes: spin-selective Andreev reflection
Qing-Lin He et al., Science 357, 294 (2017)
Chiral Majorana fermion modes at the edge
QAHI: (Cr0.12Bi0.26Sb0.62)2Te3

## Slide 48: Topological spin valve for QAH edge states
heavy V-doping (5QL)
Heavy Cr-doping (5QL)
Non-doped (3QL)
Anti-parallel alignment of the magnetizations of two surfaces
Parallel alignment of the magnetizations of two surfaces
0.5 Mega Ohm
Off state
On state
See also: Mogi et al., Nat. Mater. 16, 516 (2017)
Notes: So we realize such a topological spin-valve with co-doped (Bi,Sb)2Te3 (co-doped films have sharper magnetization reversal, which is good for such a spin-valve structrue). The top surface is a 5 QL co-doped film with more V atoms, which has larger coercivity. The bottom surface is a 5 QL co-doped film with more Cr atoms, which has smaller coercive fields. The top and bottom films are separated by a 3QL non-doped (Bi,Sb)2Te3, which decouple their magnetization. We observed a perfect “zero plateau” due to anti-parallel alignment of the magnetizations of the two surfaces. The “off state” has a resistance over 20 h/e^2 (~0.5 Mega Ohm) and the “one state” has a resistance of zero. (the feature around zero field in the lower right panel may come from magnetization reversal of some small magnetic domains. )

## Slide 49
Summary
QAHE has been confirmed
QAHI exhibits many novel properties to be explored

## Slide 50
Acknowledgements
Group Members:
Ke He, Xucun Ma, Lili Wang, C. L. Song, D. Zhang, X. Chen, S. H. Ji
Jinfeng Jia (Shanghai Jiao-Tong Univ.)
Transport: Yayu Wang (Tsinghua), Li Lv, Y. Q. Li (IOP)
Jian Wang (PKU)
Theory:
Shoucheng Zhang (Stanford), Bangfen Zhu, Wenhui Duan (Tsinghua), Z. Fang, X. Dai (IOP), X. L. Qi (Stanford), C. X. Liu (Penn State), Shengbai Zhang (RPI), X. C. Xie (PKU), S. Q. Shen (Hong Kong), Feng Liu (Utah)
$$$: NSF, MOST, MOE of China, CAS

## Slide 51
Thank you very much!